**Specification of McMahons Concrete Products Ltd Concrete Mix**

The dimensions and shape of the tank are per the attached drawing Exhibit 1.

The tank is composed of concrete comprised of the following standard mix:-

Stone = 800kg – 3/8 “ Clean Chip – Conforms to EN206 – 1:2002 – See Exhibit 2.

Sand = 400kg – 2mm Plastering Mortar Sand – conforms to I. S. EN – 13139:2002 –see exhibit 3

Cement = 240kg – Portland Cement CEM1 42, 5R conforms to EN197-1:2011. See Exhibit 4

Water approx. = 110 litres

Enduro HPP45 fibres – 3.25Kg - Macro Synthetic Reinforcing Fibre –conforms to EN 14889-2:2006 Part 2 See Exhibit 5.